
Supplementary Material: Novel Multiphase CO2 Photocatalysis System Using N- TiO2/CNCs and CO2 Nanobubble



**Figure S1** Methanol product after 6 hours of photocatalytic reaction using N-TiO2/CNCs for 6 hours under UV light irradiation.

**Table S1** Methanol product after 6 hours of photocatalytic reaction using N-TiO2/CNCs for 6 hours under UV light irradiation.

|  |  |
| --- | --- |
| Reaction Time (h) | Methanol Yield  (mmol/g catalyst) |
| 1 | 1.97 |
| 2 | 2.72 |
| 3 | 1.54 |
| 4 | 1.85 |
| 5 | 1.46 |
| 6 | 1.13 |